PRINT TROUBLESHOOTING PICTORIAL GUIDE

This guide assumes a basically properly built and calibrated printer http://www.reprap.org/wiki/Main_Page.

If you have not read through and attempted a complete calibration, see the REPRAP wiki for calibration instructions http://www.reprap.org/wiki/Calibration.  Some common calibration issues as well as common build related issues however are discussed.

The following categories are used identified by either print defects or by cause (if known):

<list to be put in sidebar with links to section>

CAUSES:

Material Feed

excessive

insufficient

intermittent

Extruding Temperature

too hot

too cold

Clogged Extruder

Bed Adherence

insufficient

excessive

Print Speed

too high

too low

Calibration

circularity

scale

Skipping Steps

Part Temperature

too hot

too cold

PRINT DEFECTS:

Surface Defects

Holes

small single filament

large area of filament

Waviness

Solidity of surface

Strings

Blobs

Fineness of Detail

Filaments not Touching

Body Defects

Warping

while printing

after printing

Stepping/Offsetting

Interlayer Delamination

Failure at Height

Overall Disaster

...

Bed Adherence

#0001, bed adherence, insufficient

01

PROBLEM                              		    COMMON CAUSE                   			  CORRECTION

| Prints do not adhere to build platform | Print head too high to push plastic against build platform | Change height settings, calibrate bottom stop, level build platform |
| --- | --- | --- |
|  | Build platform not clean | Clean using rubbing alcohol or amonia, or reapply surface tape |
|  | Build platform temp too low (other than PLA) | Raise build platform temp (max ~65C) |

#0002, bed adherence,...

...

#0003, Part Temperature, too hot

01								02

PROBLEM                              		    COMMON CAUSE                   			  CORRECTION

| Prints warp at height | Part temperature builds up as part is built | Change settings to turn off or down temp of heated build platform after base layers are complete. Ex: with heat on all through print and off upon print start (starting at full temp but cooling as it goes) (pic01). |
| --- | --- | --- |
|  |  | Reduce print speed to allow time to cool down. |
|  |  | Introduce wait states/orbit for each layer. |
|  |  | Add fan to reduce heat of part. |

...