PRINT TROUBLESHOOTING PICTORIAL GUIDE

This guide assumes a basically properly built and calibrated printer http://www.reprap.org/wiki/Main_Page.
If you have not read through and attempted a complete calibration, see the REPRAP wiki for calibration instructions http://www.reprap.org/wiki/Calibration. Some common calibration issues as well as common build related issues however are discussed.

The following categories are used identified by either print defects or by cause (if known):
<list to be put in sidebar with links to section>
CAUSES:

Material Feed
excessive
insufficient
intermittent
Extruding Temperature
too hot
too cold
Clogged Extruder
Bed Adherence
insufficient
excessive
Print Speed
too high
too low
Calibration
 circularity
scale
Skipping Steps
Part Temperature
too hot
too cold

PRINT DEFECTS:

Surface Defects
Holes
small single filament
large area of filament
Waviness
Solidity of surface
Strings
Blobs
Fineness of Detail
Filaments not Touching
Body Defects
Warping
while printing
after printing
Stepping/Offsetting
Interlayer Delamination
Failure at Height
Overall Disaster

...
Bed Adherence

#0001, bed adherence, insufficient

01
       PROBLEM	COMMON CAUSE	CORRECTION
Prints do not adhere to build platform	Print head too high to push plastic against build platform	Change height settings, calibrate bottom stop, level build platform
	Build platform not clean	Clean using rubbing alcohol or amonia, or reapply surface tape
	Build platform temp too low (other than PLA)	Raise build platform temp (max ~65C)

#0002, bed adherence,...

...

#0003, Part Temperature, too hot

01	02
       PROBLEM	COMMON CAUSE	CORRECTION
Prints warp at height	Part temperature builds up as part is built	Change settings to turn off or down temp of heated build platform after base layers are complete. Ex: with heat on all through print and off upon print start (starting at full temp but cooling as it goes) (pic01).
		Reduce print speed to allow time to cool down.
		Introduce wait states/orbit for each layer.
		Add fan to reduce heat of part.

...